TF Dry

Bardahl TF Dry is a concentrated synthetic lubricant scientifically compounded for dry lubrication and extreme pressure, based on Teflon basis. It reduces friction and prevents sticking. It is an unique all-purpose lubricant for numerous applications. After application it dries instantly leaving a dry, non-oily, clean, PTFE-powder surface, the slipperiest substance known to science. This product will function under a wide variety of conditions, ranging from cryogenic temperatures to 260°C or higher. Bardahl TF Dry is InS registered 1797275.

The problem

Assembly of equipment with close tolerances requires lubricant, which will not be scraped off during break in. Normal oils and greases, even ones containing graphite of molybdenum-disulfide, do not adequately meet this specialized requirement.

Chains and conveyors need a lubricant with high penetrating and corrosion resistant properties, as well as one which contains a minimum level of oil or slow evaporating solvent in order to prevent “fling off” and attraction of grime to lubricated parts.

Certain industrial applications require not only good lubrication but also the ability of the lubricant to remove existing grime to maintain or improve performance.

The working

Bardahl TF Dry will form an effective lubricating surface on any material - wood, metal, leather, plastic, elastomers, fibers, glass, etc. A thin coating can easily be applied by the aerosol package. The lubricating protecting film is very thin, very adhesive, non-oily and will penetrate in the smallest places. It has an extremely low friction coefficient and will therefore reduce “stick-slip” problems to a minimum.

Characteristics

- Is a non-oily clean dry lubricant.

- Dries very fast and leaves no oil film or wax.

- It will not collect dirt or dust.

- Resists corrosion by acids or alkali’s.

- Will not be affected by water, oil or solvents.

- Prevents materials sticking in molds, bins, tanks, etc.

- Will not melt or freeze.

Directions to use

Apply Bardahl TF Dry on a clean and dry surface. Adhesion can be improved by controlling surface roughness, especially important with air-dried coatings that are exposed to high shear forces in applications such as metal extrusion.

Properly applied a “tf-dry” coating will not be effected by water or other material with which they come in contact.

The product will dry in about 4 minutes at room temperature. Raising the air temperature can reduce drying time.

Applications

- Sliding mechanisms, nuts, bolts, cables, tools, conveyors - anywhere a dry powder lubricant is required up to 260°C.

- For lubricating pump-shafts and valve stems just prior to installing packing, and in the installation of flange gaskets for easier disassembly.

- As breaking-in lubricant for packings (prevents sticking). A light coating on the wearing surfaces of the packing and shaft will provide extra protection during critical start-up period of newly installed packing.

- For conveyers, slides, mechanisms requiring a non-staining lubricant.

- For drawer sliding surfaces and windows.

Removal of coating

A Bardahl TF Dry coating can be loosened with solvent and than be removed with a cloth or brush.

Typical properties of Bardahl TF Dry

Chemical structure			PTFE dispersion,  polymers in alcohol solvents

Color			 		White / transparent

Smell			 		Alcohol

Recommended temp ºC 		-80 to 260

Max. temperature, ºC 		300

Skin forming (min)			1

Curing time @20°C, 		min	5

Propellant				Propane/Butane

SG (20 º C), g/ml			0,604 g/ml

Pressure (20ºC), Bar		4,8

quantity (20ºC), g/sec		1,2

NSF approval; regnr 139796 H2.

Article number	72904

Contents		400 ml